Product	Name	Organoid® MOUS HELLGRIAN on HPL	
	Article number	MOSHGR0085HPLST	
Producer	Address	ORGANOID TECHNOLOGIES GMBH
Nesselgarten 422 / Top 5
A-6500 Fließ
Österreich
	
Description and Applications	Name	Organoid® MOUS HELLGRIAN on HPL	
	Description	Natural plant material in full coverage on engineered wood panels – HPL
produced climate neural in Tyrol, Austria	
	Applications	As a component in wood-working
	
Plant Material and Density	Plant material	Light green moss	
	Density	full coverage
	
Format und Gewicht	Format	1.320 mm x 3.050 mm	
	Gesamtstärke	1,6 mm	
	Gewicht	2.1 kg/m²

Product Requirements	Food safety	Binding agent safe for usage in contact with food in accordance with EU-regulation 1935/2004
	
Backing Material	Material	HPL engineered wood	
	Properties	Robust and durable	
	Requirements	HPL in accordance with DIN EN 438 and ISO 4586
Bulk density > 1.4 g/cm³
thermosetting plastic
food safety in accordance with EN 1186
No toxic compounds based on
antimon, barium, cadmium, chromiumIII, chromiumIV, lead, mercury, selenium
formaldehyde emission < 0.4 mg/h m2 (test: EN 717-2)
< 0.05 ppm (test: WIKI Prüfkammer)
does not contain PCP (Pentachlorophenol).
	
Technical Implementation	Cut	For cutting engineered wood, commonly used wood working machinery can be used. Panel saws, table saws, hand-held circular saws, jigsaws, but also CNC-milling. The usual principles and precautions apply, just like in working with any other engineered wood or laminate.
	
	Edges	Allow for imperfections 2 cm around the edges	
	How to process	Do not press at a temperature higher than 60°C
Use separating paper enclosed between hot press and surface
	
	Glue recommendations	White glue, urea resin, …	
	Pay attention to	Cut off 2 cm along the edges before processing, as the density of the natural material deviates due to the production process

Before processing, panels should be acclimatised between 1 and 3 days with the counter-balance. The back of the HPL needs to be checked for leftover materials or oils after processing and has to be cleaned carefully accordingly.

For sensitive wood-working applications, use a counter-balance (enclosed on request, 1.1 mm HPL). Symmetrical construction is recommended, which means using the same surface on the front and back side.

Store in closed, dry rooms at normal temperatures (approx. 20°C, 30-60% relative air humidity), laying on an even surface, like in a drawer system. Direct contact with the floor and sunlight need to be avoided.
	
	Verarbeitungshinweise unter:	https://organoid.corestad.com/verarbeitung/
(= current link)